CONSERVATION REPORT   				DATE:  27.3.08

RESTORER:  H. Dowding

THIS REPORT IS AN UPDATE OF REPORT MADE 5.3.96 BY R. HOWELLS

LOCATION/OWNER:  National Trust, Dynevor Castle

MUSEUM NO:  TH/P/37L

TITLE/ARTIST:  Old Dynevor Castle/Unknown artist

DIMENSIONS:  859mm (h) x 1250mm (w)

FRAME DIMENSIONS:  unframed for examination

INSCRIPTIONS:  As 1996.

FRAME:  Black painted wood display frame, probably nineteenth century

FITTINGS: Brass mirror plates

GLAZED:  4.4mm laminated low reflective glass

BACKBOARD:  Melinex backing with brown gummed paper tape dust seal

CONDITION:  Fair condition, fairly rigid with a few small scrapes and dents to the black painted coating

SUPPORT:

CANVAS:  The canvas has been lined and the tacking edges cut off so examination of the original was not possible.  However, on the x-radiograph, the canvas can be seen to be a medium/coarse plain weave canvas with cusping all round indicating that it has probably not been cut down significantly.

X-radiograph

Bull		       Blue lady		   Red lady

The x-radiograph shows up paint losses in the original paint and ground as dark patches, these are mainly around the edges.  The slightly x-ray denser patches where the figures and the bull are positioned are indicated above.  Otherwise, any further detail in the x-radiograph is masked by the strong absorption of the ground with the broad pattern of arc-shaped scrapes relating to the application of the ground.  See PRIMING below.

STRETCHER: 7-member stretcher

WEDGES:  All wedges present, and tied in with fishing wire and screws.

LINED:  Yes, probably glue-paste (rather than wax, as supposed in 1996), the lined canvas is very stiff.  The lining canvas is adhered to the back of the stretcher.

ATTACHMENT TO STRETCHER: Rusty iron tacks on sides, evenly spaced.

SLACK:  No, the tension is good.

HOLES:  None apparent.

TEARS:  All four corners torn slightly.  Tear in right hand turnover edge, 48mm up, 35mm long.  Although the tension is currently good, these tears should be repaired to prevent further deterioration and loss of tension in the corners.

DENTS/BULGES:  None apparent.

WOODWORM:  None apparent.

CONDITION:  Back of canvas and stretcher dusty and dirty – worst behind stretcher bars.  Scratches and gouges on back of stretcher.  Residues of gummed tape on keys.

There is canvas cusping visible at the left, right and lower edges.  It is not visible at the top because of the thickness of the paint.

PRIMING

A layer of grey priming appears to lie directly on the sized canvas.  This appeared to consist of two layers, a lower white layer and a second grey layer containing white and black pigments, though the ground was so soft and crumbly it was not possible to take a good cross section of all the layers to confirm this. See report by Libby Sheldon.  The cross section photographs show the top layer of ground, including small black pigments, the lower layer of ground is missing from the cross section.  This type of ground seems quite common for the time, Kate Stonor has noted this in the seventeenth century works at the Courtauld Gallery, London and Tate Gallery, London, see Appendix 1.   Arc shaped streaks visible in the x-radiograph appear to relate to the application of the first priming layer with a palette knife.  She found that the first layer would consist mainly of a chalk rich oil layer, then a thinner grey priming composed of lead white and charcoal black, in TH/P/38L, Libby thought that the black was likely to be lamp black.  The thin lead white rich second layer would get caught in the grooves left by the palette knife in the lower layer giving rise to the x-ray dense lines.  The pigments present in the lower layer of ground on this painting have not been confirmed by analysis.

PAINT FILM: Probably oil (not tested)

The paint film appears to have been applied in one or two thin layers.  The sky and landscape including the trees appear to have been applied directly over the ground with highlights of the trees applied on top.  The trees appear formulaic as if applied with a specially made brush with the highlights of the trees similarly applied with a specially made arc shaped brush.

Examination by x-radiography, ultra-violet light, infra red and visual examination under the microscope showed no major changes.  The sky appeared to be a mixture of lead white and smalt.  The x-radiograph of this painting shows the sky to be less x-ray opaque than the landscape and castle which is the reverse to what one would expect.

Detail of x-radiograph, mid RHS.

Sky

Castle

Trees

The sky was abraded and almost completely overpainted but not as much as the view of Newton House with the red man.  The mid green landscape was a mixture of blue/green verditer, smalt, yellow orpiment, earth colours, possibly including an orangey earth pigment and lead white.  It appeared brown in certain areas probably because a copper resinate glaze has been used, this is a glaze that is bright turquoise green when applied but discolours brown over time. This glaze has been abraded on the tops of the canvas weave.  Nearer to the sky, where the landscape is pale greeny grey, smalt particles are included in the paint film.

The trees were generally either blue/green verditer, orpiment, red and white with a discoloured copper resinate glaze, or those that appear completely brown had less of the blue/green verditer layer, more brown pigment that may be earth pigment with a discoloured copper resinate glaze or just copper resinate alone.  Highlights of the trees appeared to contain more blue/green verditer, black, red earth and orpiment and had less copper resinate glaze.

Both blue and red ladies appeared to have been originally painted over the green verditer mixture of the landscape.  They had been subsequently heavily overpainted with a similar coarse grained overpaint to that of the green overpaint over the red figure in painting TH/P/38L, except there was no intervening landscape colour.  This coarse grained overpaint was cracked and abraded and had been crudely repainted again in yet more overpaint under the natural resin varnish.  More overpaint had subsequently been applied on top of this varnish, under the synthetic varnish, as can be seen showing as the dark patches in the detail of the ultra violet light photograph shown below.

Detail of ultra-violet light photograph.

Overpaint on top of varnish

However, small patches of original paint could be seen, particularly in the faces, that indicated that the figures were part of the original composition.  This also appeared to be the case for the bull.

The river appears to have been a mixture of smalt, orpiment and white.  In some areas there were almost no blue coloured pigments visible, just the occasional orpiment particle, although the overpaint was so extensive it was difficult to find any original visible.  An abraded Prussian blue or ultramarine overpainted glaze was present over the original, and further layers of overpaint with no visible particles under magnification of 43.75x.

Photographs taken through microscope, please refer back to the photograph of the whole painting.

a) Sky, 43.75 x magnification.

Smalt

Red pigment particle, possibly red earth (?)

Abraded, discoloured copper resinate glaze (?)

Blackish glaze particles in overpaint

b) Sky, 43.75 x magnification

Smalt

Discoloured, abraded, copper resinate leaves

Abraded, discoloured copper resinate glaze

Blackish glaze particles in overpaint

b) Sky, 43.75 x magnification

Discoloured, abraded, copper resinate leaves

Abraded, discoloured copper resinate glaze

Black glaze particles in overpaint

Smalt

c) Distant landscape, 43.75 x magnification

Green verditer

Discoloured, abraded, copper resinate glaze

Smalt

d) Faded distant landscape, 43.75 x magnification

Transparent pale blue/grey particles

Orpiment

Blackish glaze particles in overpaint

Brown earth pigments (?)

Blue/green verditer

e) Between clump of trees, LHS, 43.75 x magnification

Smalt

Blackish glaze particles in overpaint

Blue/green verditer

Orpiment

f) Trees in middle distance, LHS, 43.75 x magnification

Blackish glaze particles in overpaint

Blue/green verditer

White

Earth red

Orpiment

Earth yellow

g) Mid green landscape, LHS, 43.75 x magnification

Blue/green verditer

Blackish glaze particles in overpaint

Orpiment

White

h) Dark green of trees in wood, 43.75 x magnification

Ground

Blue/green verditer

Blackish glaze paticles in overpaint

Discoloured copper resinate

h) Dark green of trees in wood, 43.75 x magnification

Blue/green verditer

Earth pigments (?)

Ground

Infra red examination did not reveal any underdrawing or changes to the image, but did show the details of the figures and the bull in slightly greater clarity than in the actual painting

OTHER:  Not tested.

CRACK TYPES: All over age craquelure, the paint surface is very broken up with brittle age cracks.  Weave emphasis also makes the canvas texture very noticeable.  Both factors affect the texture of the painting and make the image difficult to read because of the reflections from the different textures

FLAKING: None apparent.

LOSSES: Lots of tiny old losses, generally not filled or retouched, but under the varnish.

OVERPAINT:  Extensive.  In the centre of the lower edge, there is a strip of tape, probably left from before the original tacking margins were cut off and the painting lined.  The tape is partially covered with paint, which confirms that there is overpaint in this area.  The sky is almost completely overpainted.  At the left hand side, the top part of the section of lining canvas that is visible has also been painted, possibly because it was visible when the painting was framed.  There is similar paint level with the hill section of the right hand side.

UV showed that the majority of the overpaint is under the varnish.  A pea green fluorescence indicates a natural resin varnish.  There are some dark patches over this varnish, with lots of brushstrokes reinforcing leaves at the edges of the trees.  There is some retouching to the bull over the varnish.  There is a dark patch around the head of the left-hand figure.  There is a pale vertical stripe c.200mm in from the left in UV.  This does not seem to be a band of retouching.  There is an overall synthetic varnish.

BLOOMED OR BLANCHED: See 1996 report.

CONDITION:  Stable.  Lots of lumps across the surface – probably slubs in the canvas.  There are lots of bristles/hairs in the paint or varnish.

VARNISH:

DISCOLOURED:  Not significantly

DISFIGURING:  See PATCHY.

PATCHY:   Varnish has uneven gloss, and light is scattered by the surface texture, making it appear patchy and difficult to read.

MOULD:  None apparent.

BLOOMED OR BLANCHED:  None apparent.

SURFACE DIRT: Some dust and dirt deposits

Rachel Howells

Painting conservator

28.05.08