CONSERVATION REPORT   				DATE: 27.3.08

RESTORER:  H. Dowding

THIS REPORT IS AN UPDATE OF REPORT MADE 5.3.96 BY R. HOWELLS

LOCATION/OWNER:  National Trust, Dynevor Castle

MUSEUM NO:  TH/P/36L

TITLE/ARTIST:  Newton/Unknown artist

DIMENSIONS:  838mm (h) x 1277mm (w)

FRAME DIMENSIONS:  unframed for examination

INSCRIPTIONS:  See 1996 report.

FRAME:  Black painted wood display frame

FITTINGS:  Brass mirror plates

GLAZED:  4.4mm laminated low reflective glass

BACKBOARD:  Melinex backing with gummed paper tape dust seal

CONDITION:  Fair condition, fairly rigid, a few small knocks and scrapes to the black painted coating.

SUPPORT:

CANVAS: The original canvas has been lined but the weave of the original can be seen in the x-radiograph and at the cut edges to be medium /coarse plain weave.  Examination of the cusping around the edges in the x-radiograph indicates that the sides do not appear to have been cut down.  As the painting depicts houses on a slant, there was a question as to whether the top and bottom edges had been cut at a slant, yet the cusping along the bottom edge does not show this.  At the top, there is slightly less cusping towards the lhs, but any additional canvas in this area would give the painting even more of a slant.

X-radiograph

STRETCHER:

WEDGES:  One missing, lower rhc (from back), one broken off at the bottom cross bar, all others secured with fishing line.

LINED:  Probably glue-paste (not wax, as suggested in 1996 – unframed examination revealed remnants of glue-paste around edges of original canvas).

ATTACHMENT TO STRETCHER:  Rusty iron tacks, evenly spaced, on sides.  Lining canvas adhered to back of stretcher.

SLACK:  No.

HOLES:  None apparent.

TEARS:  All corners slightly torn.

DENTS/BULGES:  None apparent.

WOODWORM:  None apparent.

CONDITION: Stable.

PRIMING

A layer of grey priming appears to lie directly on the sized canvas.  This appeared to consist of two layers, a lower white layer and a second grey layer containing white and black pigments, though the ground was so soft and crumbly it was not possible to take a good cross section of all the layers to confirm this. In the cross section photographs included in the report by Libby Sheldon, the top layer of ground with fine black pigments in it can be seen, but the lower layer is missing.  This type of ground generally seems quite common for the time, Kate Stonor has noted this in the seventeenth century works at the Courtauld Gallery, London and Tate Gallery, London, see Appendix 1.   The arc shaped streaks visible in the x-radiograph appear to relate to the application of the first priming layer with a palette knife.  She found that the first layer would consist mainly of a chalk rich oil layer, then a thinner grey priming composed of lead white and charcoal black, in TH/P/38L, Libby thought the black was likely to be lamp black.  The thin lead white rich second layer would be caught in the grooves left by the palette knife in the lower layer giving rise to the x-ray dense lines.  The pigments in the lower ground on this painting have not been confirmed by analysis.

PAINT FILM:  Probably oil (not tested).

The paint film appears to have been applied in one or two thin layers.  The sky and landscape including the trees appear to have been applied directly over the ground with highlights of the trees applied on top.  The trees appear formulaic, the highlights of the distant trees have probably been applied with a specially made arc shaped brush, the arrow head trees appear to be  be discoloured copper resinate with a single stroke of a mixture of blue/green verditer, orpiment and white for the highlight.  Examination by x-radiography, infra red and visual examination under the microscope showed no major changes.  The sky appeared to be a mixture of lead white and smalt.  The x-radiograph of this painting shows the sky to be more x-ray opaque than the landscape and castle which is as one would expect.  The mid green landscape, and the formal garden, were a mixture of blue/green verditer, smalt, yellow orpiment, earth colours, possibly including an orangey earth pigment and lead white.  It appeared brown in certain areas because of a brown glaze that may be copper resinate, once a turquoise coloured glaze, now discoloured brown. This glaze has been abraded on the tops of the canvas weave.  Nearer to the sky, where the landscape is pale greeny grey, smalt particles are included in the paint film.

The trees were generally either blue/green verditer, orpiment, red and white with a discoloured copper resinate glaze, or those that appear completely brown had less of the blue/green verditer layer, more brown pigment that may be earth pigment with a discoloured copper resinate glaze or just copper resinate alone.  Highlights of the trees appeared to contain more white, blue/green verditer, black, red earth and orpiment and had less copper resinate glaze.  The highlights of the arrow shaped trees at the bottom lhc contained a mixture of blue/green verditer and orpiment.

The tower appeared to have been painted using a transparent brown with red and yellow earth pigments, blue/green verditer, black, white and orpiment.  The brownish looking foliage appears likely to be a discoloured copper resinate, much of this is abraded and missing/or overpainted so that the tower now appears to have less surrounding foliage than it would have had.

The small pink buildings on the right appear to have been painted over the blue/green verditer containing colours of the landscape and contain red, white and black pigments.

The line of the roof of the house has been painted over the trees.

Paint samples were taken from the sky (3), the mid green landscape and the dark green of the trees to be looked at in cross section.

Overall view, showing sample sites for cross section analysis

Sample 3.	Sample 4.	   Sample 1.       Sample 5.   Sample 2.

Sample 1. taken from the bottom edge of the loss.

43.75 magnification

Overpaint with red and blue particles

Original sky with smalt particles

Canvas thread

Sample 2. taken from the bottom edge of the loss.

43.75 magnification

Blue black overpainted glaze – Prussian

blue/ultramarine?

Smalt particles

Canvas thread

Grey priming

Sample 3. Mid green landscape next to highlight

7.5 x magnification	       43.75 x magnification

Shiny yellow

Smalt

Blue/green verditer

Priming

Canvas thread

Sample 4.  Dark green trees, sample taken from the edge of the loss.

7.5 x magnification	           43.75 x magnification

Shiny yellow

Blue/green verditer

Discoloured copper resinate

glaze.

Canvas thread

Sample 5.  Sky at the top edge.

43.75 x magnification

Over paint with red, blue and white particles

Original blue sky with smalt particles

Overpaint with no discernable particles

PIGMENT ANALYSIS

For a full description of pigments found in the samples please refer to the report on the Technical Analysis by Libby Sheldon, pp 5 - 6, and to the description of the PIGMENT ANALYSIS in the conservation report of TH/P/38L.

CRACK TYPES: All over age craquelure, more evident in the dark shadows.

FLAKING:  None apparent.

LOSSES:  Frame rebate damage, upper part of right hand side.  The x-radiograph shows substantial loss to the bottom of the sides and numerous discreet losses in the bottom half of the painting show as dark patches.  Numerous small unfilled unretouched losses were present all over the painting.

OVERPAINT:  Extensive.  Sky almost completely overpainted, at least two layers of overpaint were visible with a dark blue, ultramarine or Prussian blue glaze under the overpaint layers.

The ultraviolet photograph below shows the most recent layer of overpaint in the sky as a dull, purplish fluorescing layer, underneath that is a brighter blue fluorescence from the lower layer of overpaint, other recent retouchings on top of the natural resin varnish are visible as dark patches in the foreground and in the buildings.

Whole view in ultra –violet light

The infra red examination did not reveal any underdrawing but also shows the retouchings on top of the varnish as dark patches, see photo below.

Photo in infra red – detail of buildings. Overpaint on turnover edge showing as dark patches in infra red.

BLOOMED OR BLANCHED:  None apparent.

CONDITION:  Unchanged since 1996 assessment.

VARNISH:

DISCOLOURED:  No.

DISFIGURING:  Patchy.

PATCHY:  Surface gloss is disturbed by the various textures of the painting; unfilled retouchings, cupped craquelure, weave emphasis of canvas texture and a reflective varnish.

MOULD:  None apparent.

BLOOMED OR BLANCHED:  None apparent.

SURFACE DIRT: Some dusty deposit soluble in saliva.

Rachel Howells

Painting Conservator

28.05.08